# BGA Void Inspection Report

Quantitative & qualitative void analysis per IPC-A-610 / IPC-7095

| Board / image | PCBA2_03.jpg |
| --- | --- |
| Report generated | 2026-07-09 20:37 |
| Inspection tool | BGA X-ray Void Inspection Tool |
| Standards applied | IPC-A-610 / IPC-7095 |
| BGA grid / balls analyzed | 256 expected pads, 256 analyzed |

IPC VERDICT: ACCEPT WITH PROCESS INDICATORS

No IPC-A-610 defect. 5 ball(s) in the 10-25% process-indicator band; 1 ball(s) carry one dominant void (IPC-7095 process guidance).

# Key void metrics

| Average void ratio | 4.109 % |
| --- | --- |
| Median void ratio | 4.0767 % |
| Worst ball (total void) | 15.8939 % |
| Worst single void | 14.6691 % |
| Assessment split | 251 acceptable / 5 process indicator / 0 defect |

# IPC criteria evaluation

| Criterion | Source | Limit | Measured | Result |
| --- | --- | --- | --- | --- |
| Cumulative void area per ball | IPC-A-610 (Class 1, 2, 3) | <= 25% of ball area | worst ball: 15.89% | PASS |
| Process indicator band (total void 10-25%) | IPC-7095 process guidance | monitor, not a defect | 5 ball(s) in band | INFO |
| Largest single void per ball | IPC-7095 (dominant-void guidance) | review above 12.2% area (~35% diameter) | worst single void: 38.3% of ball diameter | INFO |
| Void location at pad interface | IPC-7095 (30% dia at land) | requires oblique/3D view | not measurable in one top-down 2D X-ray | NOT EVALUATED |
| Complete ball grid detected | detection integrity gate | all expected pads found | 256 / 256 | PASS |

# Worst 10 balls by total void

| Ball ID | X (px) | Y (px) | Total void (%) | Largest void (%) | IPC assessment |
| --- | --- | --- | --- | --- | --- |
| 51 | 2244 | 1130 | 15.89 | 14.67 | PROCESS INDICATOR |
| 249 | 223 | 2415 | 12.49 | 4.57 | PROCESS INDICATOR |
| 28 | 500 | 931 | 10.89 | 7.61 | PROCESS INDICATOR |
| 253 | 78 | 2408 | 10.78 | 6.54 | PROCESS INDICATOR |
| 213 | 1760 | 2178 | 10.10 | 2.45 | PROCESS INDICATOR |
| 92 | 1431 | 1307 | 9.75 | 2.34 | ACCEPTABLE |
| 120 | 1158 | 1512 | 8.97 | 2.69 | ACCEPTABLE |
| 44 | 359 | 1023 | 8.69 | 4.34 | ACCEPTABLE |
| 132 | 1870 | 1612 | 8.47 | 6.18 | ACCEPTABLE |
| 86 | 1158 | 1312 | 8.35 | 3.98 | ACCEPTABLE |

# Annotated X-ray (detected voids)

# Algorithm analysis - honest assessment

## Detection integrity

Balls detected: 256 of 256 expected grid slots

Pads placed from grid estimation (no direct evidence): 0

Mean detection confidence (evidence-backed pads): 1.00

Ball quality split: 251 PASS / 5 REVIEW / 0 FAIL

## Measurement pipeline (what actually produced these numbers)

1. CLAHE contrast enhancement + median denoising of the raw X-ray.

2. Solder-ball detection: Hough circles + dark-blob evidence, regularized onto the 16x16 BGA grid (affine + homography fit for oblique views, per-ball local snap with non-degradation gates).

3. Per-ball void segmentation: median-background subtraction (kernel > ball radius), bond-wire suppression by grayscale closing, residual threshold, then shape filtering.

4. Detected void blobs are rendered as fitted circles when they fill >= 45% of the fitted disc (physical voids are spherical gas bubbles); ragged non-circular structures keep their raw contour.

5. Component-level sanity filters remove rim arcs, trace stripes, bare-board bleed-through and empty-pad artifacts before metrics.

## Classification thresholds applied

Defect (FAIL): total void >= 25.0% of ball area (IPC-A-610).

Process indicator (REVIEW): total void >= 10.0% (IPC-7095 guidance).

Dominant single void (REVIEW): largest void >= 12.25% of ball area (~35% of ball diameter).

## Measurement uncertainty - read before trusting decimals

Projected-area measurement: one top-down 2D X-ray cannot separate package-interface, mid-ball and pad-interface voids; the 25% IPC-A-610 criterion is applied on the projection, exactly as the standard defines it for X-ray inspection.

Analysis is restricted to the inner 82% of each ball radius; a void hiding exactly on the ball rim can be underestimated.

Voids smaller than ~10 px^2 (about 0.15% of a ball) are below the detection floor and are intentionally ignored as noise.

Fitted-circle rendering slightly increases void area versus the raw threshold blob (it includes the faded bubble edge); this is closer to the physical bubble size but adds ~0.3-0.6 percentage points to board averages compared to raw-contour reporting.

JPEG compression artifacts and CLAHE amplification set a noise floor around 1-2% void ratio; differences below that level are not meaningful.

On oblique views, perspective foreshortening distorts both ball and void areas; the ratio is partially self-correcting but not perfectly.

## Known limitations of this analysis

Components mounted on the opposite board side project dark shadows between and over balls; the detector anchors circles on grid geometry to resist this, but heavily shadowed balls have reduced void sensitivity.

Grid slots occupied by vias (no ball populated) are still reported as balls when the slot must be filled; they show ~0% void and near-board brightness.

Bond-wire suppression (morphological closing) can mask very thin elongated voids lying exactly under a wire.

The tool measures voiding only; it does not assess head-in-pillow, non-wet opens, bridging or solder-ball shape defects.

## Balls to verify manually first (worst 10 by total void)

Ball # 51 at (2244, 1130): total 15.89%, largest single 14.67% -> PROCESS INDICATOR

Ball #249 at (223, 2415): total 12.49%, largest single 4.57% -> PROCESS INDICATOR

Ball # 28 at (500, 931): total 10.89%, largest single 7.61% -> PROCESS INDICATOR

Ball #253 at (78, 2408): total 10.78%, largest single 6.54% -> PROCESS INDICATOR

Ball #213 at (1760, 2178): total 10.10%, largest single 2.45% -> PROCESS INDICATOR

Ball # 92 at (1431, 1307): total 9.75%, largest single 2.34% -> ACCEPTABLE

Ball #120 at (1158, 1512): total 8.97%, largest single 2.69% -> ACCEPTABLE

Ball # 44 at (359, 1023): total 8.69%, largest single 4.34% -> ACCEPTABLE

Ball #132 at (1870, 1612): total 8.47%, largest single 6.18% -> ACCEPTABLE

Ball # 86 at (1158, 1312): total 8.35%, largest single 3.98% -> ACCEPTABLE

## Grid-estimated pads (verify visually)

None - every pad was detected from direct image evidence.

Generated automatically by BGA X-ray Void Inspection Tool on 2026-07-09 20:37. Verdicts follow IPC-A-610 (25% cumulative projected void area per ball) with IPC-7095 process guidance; they are based on a single top-down 2D X-ray projection and should be confirmed by an operator for boards flagged REVIEW or REJECT.